-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep42ht-4aomed-black .

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Medical Grade Epoxy Offers Thermal Conductivity and Electrical Insulation

Master Bond EP42HT-4AOMed Black is a new two part epoxy created for medical device manufacturing. It is biocompatible and non-cytotoxic, passing both USP Class VI and ISO 10993-5 certifications. This epoxy withstands aggressive chemical sterilants, radiation and repeated cycles of autoclaving.

EP42HT-4AOMed Black offers both cryogenic serviceability and heat resistance with a service temperature range from 4K to 400°F. Its thermal conductivity measures 9-10 BTU•in/(ft2•hr•°F) and its volume resistivity is greater than 1014 ohm-cm. The system contains a filler, which contributes to its high strength profile and dimensional stability. This adhesive bonds well to metals, composites, glass, ceramics, rubbers and plastics and features a tensile modulus of 500,000-550,000 psi, a compressive strength of 24,000-26,000 psi, and a tensile strength of 7,000-8,000 psi.

This epoxy can cure at room temperature, yet faster cures can be achieved by heat curing. In order to obtain optimal properties, an overnight cure at room temperature, followed by heat curing at 150-200°F for 2-3 hours is recommended. The mix ratio is 100 to 40 by weight. Once mixed, this versatile adhesive has very good flow properties, making it suitable for bonding, sealing and coating applications. Upon curing, EP42HT-4AOMed Black exhibits very low shrinkage, low exotherm and can be used for castings up to 2-3 inches thick. This opaque black epoxy is available in the following size kits: ½ pint, pint, quart and gallon. It is also available in pre-mixed and frozen syringes, which are compatible with automated dispensing equipment.

Master Bond Medical Adhesive Systems

Master Bond EP42HT-4AOMed Black is a two component epoxy adhesive system developed for medical device applications. It passes USP Class VI and ISO 10993-5 certifications and successfully resists multiple sterilization methods. Read more about Master Bond’s adhesives, sealants and coatings for medical device manufacturing at https://www.masterbond.com/industries/medical-adhesives-sealants-and-coatings or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/https://www.masterbond.com/newsrelease/ep42ht-4aomed-black .

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #