The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/mastersil-972tc-lo.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Thermally Conductive, Electrically Insulative Two Part Silicone Meets NASA Low Outgassing Specifications

Master Bond MasterSil 972TC-LO passes the rigorous requirements for low outgassing per ASTM E595 specifications. It is particularly well suited for use in vacuum environments as well as applications in the aerospace, electronic, opto-electronic and specialty OEM industries. This two part silicone system offers convenient handling for bonding, sealing, coating and potting.

MasterSil 972TC-LO is an electrically insulator that has a thermal conductivity of 7-9 BTU•in/ft²•hr•°F [1.01-1.30 W/(m•K)]. It bonds well to a wide variety of substrates, including metals, composites, glass, ceramics, rubbers as well as many types of and plastics. Highly flexible, MasterSil 972TC-LO has an elongation of 40-80%, withstands aggressive thermal cycling and resists mechanical shock. This heat dissipative silicone system has a wide service temperature range is -120°F to +400°F.

This addition cured system does not require air for cross-linking. It features low shrinkage upon curing even in thick or wide cross sections. MasterSil 972TC-LO has a moderate viscosity of 30,000-40,000 cps with good flow properties and has a one to one mix ratio by weight. It has a long working life of 6-10 hours at room temperature. This compound is 100% solids and has a white color. Mastersil 972TC-LO is available in 50 gram syringe kits with additional sizes upon request.

Master Bond Low Outgassing Adhesives

MasterSil 972TC-LO is high temperature resistant, thermally conductive system offers excellent flexibility and elongation. This two part silicone also passes NASA low outgassing requirements. Read more about Master Bond’s low outgassing adhesives at http://www.masterbond.com/certifications/nasa-low-outgassing or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/mastersil-972tc-lo

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #