-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/supreme-3htnd-2da.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Thermally Conductive, Electrically Insulative One Part Epoxy for Die Attach Applications

Formulated for die attach applications, Master Bond Supreme 3HTND-2DA is a fast curing, high performance one component epoxy system. It cures in 5-10 minutes at 150°C and has unlimited working life at room temperature. It is available in syringes and has a shelf life of 6 months when stored at 40-50°F.

Supreme 3HTND-2DA has a die shear strength of 19-21 kg-f and performed very well in 85/85 testing. This epoxy has excellent adhesion to metals, ceramics and silicon dies. It is serviceable over the wide temperature range of -100°F to+400°F. As a toughened system, it offers the ability to withstand rigorous thermal cycling and shock.

In accordance with die attach application requirements, this product passes NASA low outgassing test specifications. Supreme 3HTND-2DA has low ionics, particularly chlorine (<15 ppm). It also features dimensional stability, superior thermal conductivity, electrical insulation properties and a glass transition temperature of 100-105°C.

Unlike many other die attach systems, Supreme 3HTND-2DA is not premixed and frozen, but it requires refrigeration for storage. This system dispenses smoothly or without any tailing. It well suited for automatic dispensing equipment. With a viscosity of over 300,000 cps (thixotropic), it can be applied to a defined area without running.

Master Bond Toughened Epoxy Compounds

Master Bond Supreme 3HTND-2DA is a NASA low outgassing system for die attach applications featuring thermal conductivity, high temperature resistance and toughness. Read more at http://www.masterbond.com/properties/flexibilized-and-toughened-adhesive-systems or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/supreme-3htnd-2da

Check out more videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #