The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/uv22dc80-1med.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Dual Curing Epoxy Meets Biocompatibility and Cytotoxicity Requirements

Master Bond UV22DC80-1Med is a single component, nanosilica filled compound featuring a UV and heat curing mechanism. Not only does it pass USP Class VI tests for biocompatibility, but it also meets ISO 10993-5 for cytotoxicity, making it ideal for many applications in the medical device industry.

As a nanosilica filled system, UV22DC80-1Med offers low shrinkage upon cure, excellent abrasion resistance and dimensional stability with a low coefficient of thermal expansion of 30-35 x 10-6 inch/inch/°C. It is a reliable electrical insulator with volume resistivity of more than 1014 ohm-cm and dielectric constant of 3.85 at 60 Hz.  UV22DC80-1Med is optically clear with a refractive index of 1.52.

The UV curing process for UV22DC80-1Med takes only 10-30 seconds at a 365nm wavelength and 10-40 mW/cm2 of UV output. The heat curing process can be initiated at 80°C, making it highly desirable in applications involving heat sensitive components. Optional post curing at 125-150°C for 15-30 minutes will increase the glass transition temperature to over 125°C.This system is not oxygen inhibited.

UV22DC80-1Med has a low viscosity of 500-3,500 cps at 75°F (~ 23°C). It bonds well to a variety of substrates including metals, glass, ceramics and most plastics. This compound has very good resistance to various sterilization methods including autoclaving and many chemical sterilants. It is available for use in 30 cc EFD syringes, ½ pint, pint, and quart containers.

Master Bond Biocompatible Adhesives

Master Bond UV22DC80-1Med is a one part dual UV and heat cure system that meets USP Class VI and ISO 10993-5 requirements. It features optical clarity, abrasion resistance and dimensional stability. Read more about our biocompatible adhesives at https://www.masterbond.com/properties/biocompatible-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/uv22dc80-1med

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #